## Slide 1: Outline
Introduction
Material and Methods
2.1 Lab-scale BMED Stack
The figure of setup
2.2 Protocol
2.3 Scaling Characterization and BMED Performance Analysis
2.3.1 Scaling characterization
SEM, EDS, XRD, turbidimeter
Calculation of scaling(RMg, RCa, mass of scaling)
2.3.2 BMED Performance Analysis
Conductivity, voltage, pH
Energy consumption
SI

## Slide 2
3. Results and Discussion
3.1 Scaling in BMED
3.1.1 Scaling characterization in BMED system
  When treating NaCl, there is no scaling SEM and EDS
  When treating SWB, there is severe scaling in the chamber and membrane
    Chamber  Turbidity before and after experiments
    Membrane  photo of membranes after experiments
  Explore the scaling formation mechanism
    Where scaling is formed  SEM and EDS of each membrane surface/cross-section
      CEM facing SWBC
      CEM facing BC
      BPM facing BC
    What is the composition  XRD, SEM&EDS of crystal
    Why scaling is formed
      CEM facing SWBC: Water splitting (major)  pH decrease in salt chamber; OH- leakage (minor) transport number decrease (membrane deformation, crystal block…)
      CEM facing BC: divalent ion transport
      BPM facing BC: High concentration of OH-
    Conclusion

## Slide 3
3. Results and Discussion
3.1 Scaling in BMED
3.1.1 Scaling characterization in BMED system
  When treating NaCl, there is no scaling SEM and EDS
SI

## Slide 4
3. Results and Discussion
3.1 Scaling in BMED
3.1.1 Scaling characterization in BMED system
  When treating NaCl, there is no scaling SEM and EDS
  When treating SWB, there is severe scaling in the chamber and membrane
    Chamber  Turbidity before and after experiments
    Membrane  photo of membranes after experiments
SI
SI

## Slide 5
3. Results and Discussion
3.1 Scaling in BMED
3.1.1 Scaling characterization in BMED system
  When treating NaCl, there is no scaling SEM and EDS
  When treating SWB, there is severe scaling in the chamber and membrane
    Chamber  Turbidity before and after experiments
    Membrane  photo of membranes after experiments
  Explore the scaling formation mechanism
    Where scaling is formed  SEM and EDS of each membrane surface/cross-section
      CEM facing SWB, CCEM facing BC, BPM facing BC

## Slide 6
3. Results and Discussion
3.1 Scaling in BMED
3.1.1 Scaling characterization in BMED system
  When treating NaCl, there is no scaling SEM and EDS
  When treating SWB, there is severe scaling in the chamber and membrane
    Chamber  Turbidity before and after experiments
    Membrane  photo of membranes after experiments
  Explore the scaling formation mechanism
    Where scaling is formed  SEM and EDS of each membrane surface/cross-section
      CEM facing SWBC, CEM facing BC, BPM facing BC
    What is the composition  XRD, SEM&EDS of crystal

## Slide 7
3. Results and Discussion
3.1 Scaling in BMED
3.1.1 Scaling characterization in BMED system
  When treating NaCl, there is no scaling SEM and EDS
  When treating SWB, there is severe scaling in the chamber and membrane
    Chamber  Turbidity before and after experiments
    Membrane  photo of membranes after experiments
  Explore the scaling formation mechanism
    Where scaling is formed
      CEM facing SWBC
      CEM facing BC
      BPM facing BC
    What is the composition
    Why scaling is formed
      CEM facing SWBC:
        Water splitting (major)  pH decrease in salt chamber;
        OH- leakage (minor) transport number decrease
        (membrane deformation, crystal block…)
      CEM facing BC: divalent ion transport
      BPM facing BC: High concentration of OH-
    Conclusion

## Slide 8
3.1.2 Effect of Scaling on BMED Performance
Conductivity, voltage, concentration of acid/base, pH of salt chamber, SEC
  Voltage change  membrane resistance
Reversibility testing  The necessity to mitigate scaling on membrane
SI

## Slide 9
3.2 Effect of Mono-/di-valent selectivity of CEM on scaling
Quantification of scaling
- Performance
SI

## Slide 10
3.3 Effect of current density on scaling
Quantification of scaling
- Performance
SI