## Slide 1
+
AEM
CEM/
SCEM
BPM
BPM
-
AEM
CEM/
SCEM
BPM
AEM
CEM/
SCEM
BPM
Electrode Chamber
Acid Chamber
Seawater Brine Chamber
Base Chamber
-
-
-
+
+
-
-
-
+
+
-
-
-
+
+
-
-
-
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
Acid flow
Base flow
Electrode flow
Seawater brine flow
Notes: Fig. 1 The configuration of lab-scale experimental BMED stack.

## Slide 2
10 μm
10 μm
10 μm
10 μm
Ca
10 μm
Mg
10 μm
Ca
10 μm
Mg
Ca
10 μm
Mg
10 μm
Mg
Ca
10 μm
10 μm
10 μm
a1
a2
d1
b1
c1
a3
a4
d2
d3
d4
b2
b3
b4
c2
c3
c4
AEM facing SWBC
BPM facing BC
CEM facing SWBC
CEM facing BC
Notes: Fig. 2 SEM and EDS elemental analysis of membrane surfaces. AEM facing SWBC: (a1) SEM diagram; (a2) EDS elemental mapping image of Mg; (a3) EDS elemental mapping image of Ca; (a4) EDS map spectrum. CEM facing SWBC: (b1) SEM diagram; (b2) EDS elemental mapping image of Mg; (b3) EDS elemental mapping image of Ca; (b4) EDS map spectrum. CEM facing BC: (c1) SEM diagram; (c2) EDS elemental mapping image of Mg; (c3) EDS elemental mapping image of Ca; (c4) EDS map spectrum. BPM facing BC: (d1) SEM diagram; (d2) EDS elemental mapping image of Mg; (d3) EDS elemental mapping image of Ca; (d4) EDS map spectrum. (Conditions: Feed solution = seawater brine, current density = 15 mA/cm2, cell pairs = 3, membrane = CEM. AC: acid chamber; SWBC: seawater brine chamber; BC: base chamber).

## Slide 3
10 μm
10 μm
10 μm
10 μm
Cross-section
Surface
Ca
Mg
d1
d2
d3
d4
BPM (AEL)
10 μm
10 μm
10 μm
10 μm
Cross-section
Surface
Ca
Mg
b1
b2
b3
b4
CEM
10 μm
Pristine CEM
10 μm
Mg
10 μm
Ca
10 μm
Cross-section
Surface
10 μm
10 μm
10 μm
10 μm
Ca
Mg
Pristine BPM (AEL)
Cross-section
Surface
a1
a2
a3
a4
c1
c2
c3
c4
Notes: Fig. 3 The SEM graph and EDS map spectrum of cross-section of membranes (White line is the dividing line of cross-section and membrane surface). Pristine CEM: (a1) SEM diagram; (a2) EDS map spectrum; (a3) EDS elemental mapping image of Ca; (a4) EDS elemental mapping image of Mg. CEM after experiment: (b1) SEM diagram; (b2) EDS map spectrum; (b3) EDS elemental mapping image of Ca; (b4) EDS elemental mapping image of Mg. Pristine BPM (AEL): (c1) SEM diagram; (c2) EDS map spectrum; (c3) EDS elemental mapping image of Ca; (c4) EDS elemental mapping image of Mg. BPM (AEL) after experiment: (d1) SEM diagram; (d2) EDS map spectrum; (d3) EDS elemental mapping image of Ca; (d4) EDS elemental mapping image of Mg.

## Slide 4
BPM
+
AEM
CEM/SCEM
BPM
OH-
BPM
Cl-
-
+
+
+
+
+
+
-
-
-
-
-
-
EC
AC
SWBC
BC
…
BPM
EC
OH-
H+
Scaling on CEM/SCEM
facing SWBC
Scaling on CEM/SCEM
facing BC
1
2
Ca2+
Mg2+
Na+
Ca2+
Scaling on BPM
facing BC
3
Scaling: Mg(OH)2
The leakage of OH-
Water splitting
Scaling: Ca(OH)2
The transport of Mg2+/Ca2+
Scaling: Mg(OH)2, Ca(OH)2, CaCO3
The transport of Mg2+/Ca2+
OH-
OH-
1
Mg2+
Ca2+
Na+
2
3
…
H+
OH-
H+
Water splitting
(Major)
(Minor)
Leakage
a
Mg2+
Ca2+
1
CEM/SCEM
SWBC
BC
Mg2+
Ca2+
OH-
Divalent ion transport
Precipitate on membrane surface facing BC
SWBC
BC
Scaling reduce Aeff, decreasing Ilim.
Water splitting takes place and produces OH- and H+
OH- transports through the membrane and precipitates on membrane facing SWBC
OH-
H+
SWBC
BC
Mg2+
Ca2+
2
Scaling on membrane surface
Nanoparticles in matrix
b
Nanocrystal
in matrix
Scaling
CEM/SCEM
CEM/SCEM
Water
Splitting
OH-
Mg2+
Ca2+
1
SWBC
BC
H+
Scaling on membrane surface facing SWBC attributes to water splitting as well
The scaling was enhanced
CEM/SCEM
OH-
H+
Water
Splitting
OH-
H+
Water
Splitting
OH-
Scaling
Notes: Fig. 4 (a) Schematic illustration of mechanisms of scaling generation in BMED system (EC: electrode chamber; AC: acid chamber; SWBC: seawater brine chamber; BC: base chamber). (b) The procedure of scaling formation on both sides of CEM/SCEM. (Aeff = effective membrane area; Ilim = limiting current)

## Slide 5
d
c
e
a
b
Notes: Figure 5 Quantification of scaling in BMED system. (a) Reduction ratio of Mg2+ and Ca2+ with time; (b) The amount of scaling in BMED. The concentration change of Mg2+ and Ca2+ with time in (c) AC, (d) BC and (e) SWBC. (Conditions: Feed solution = seawater brine, current density = 15 mA/cm2, cell pairs = 3, membrane = CEM. AC: acid chamber; BC: base chamber; SWBC: seawater brine chamber).

## Slide 6
a
b
f
c
g
d
e
Notes: Figure 6 (a) Conductivity changes in salt chamber and (b) Voltage changes in BMED system treating NaCl and seawater brine (SWB). (c) Concentration of generated acid and base with time. The current efficiency and energy consumption of the entire process to produce (d) acid and (e) base. (Conditions: Feed solution = NaCl or SWB, current density = 15 mA/cm2, cell pairs = 3, membrane = CEM)

## Slide 7
10 μm
10 μm
10 μm
Mg
10 μm
Ca
10 μm
Mg
10 μm
Ca
10 μm
Mg
10 μm
Ca
10 μm
Mg
10 μm
Ca
10 μm
10 μm
a1
a2
d1
b1
c1
a3
a4
d2
d3
d4
b2
b3
b4
c2
c3
c4
AEM facing SWBC
BPM facing BC
SCEM facing SWBC
SCEM facing BC
Notes: Figure 7. SEM and EDS elemental analysis of membrane surfaces. AEM facing SWBC: (a1) SEM diagram; (a2) EDS elemental mapping image of Mg; (a3) EDS elemental mapping image of Ca; (a4) EDS map spectrum. SCEM facing SWBC: (b1) SEM diagram; (b2) EDS elemental mapping image of Mg; (b3) EDS elemental mapping image of Ca; (b4) EDS map spectrum. SCEM facing BC: (c1) SEM diagram; (c2) EDS elemental mapping image of Mg; (c3) EDS elemental mapping image of Ca; (c4) EDS map spectrum. BPM facing BC: (d1) SEM diagram; (d2) EDS elemental mapping image of Mg; (d3) EDS elemental mapping image of Ca; (d4) EDS map spectrum. (Conditions: Feed solution = seawater brine, current density = 15 mA/cm2, cell pairs = 3, membrane = SCEM. AC: acid chamber; SWBC: seawater brine chamber; BC: base chamber).

## Slide 8
d
c
e
a
b
Notes: Figure 8 Quantification of scaling in BMED system (Conditions: Feed solution = seawater brine, current density = 15 mA/cm2, cell pairs = 3, membrane = CEM (baseline, BL) and SCEM. AC: acid chamber; SWBC: seawater brine chamber; BC: base chamber). (a) Reduction ratio of Mg2+ and Ca2+ in BMED system treating SWB with different membrane stack; (b) The amount of scaling in BMED system with different membrane stack. The concentration change of Mg2+ and Ca2+ with time in (c) AC, (d) BC and (e) SWBC.

## Slide 9
a
b
d
c
e
Notes: Figure 9 (a) Conductivity change in salt chamber and (b) Voltage change with different membrane stack. (c) Concentration of generated acid and base with different membrane stack. The current efficiency and energy consumption of the entire process to produce (d) acid and (e) base with different membrane stack. (Conditions: Feed solution = seawater brine, current density = 15 mA/cm2, cell pairs = 3, membrane = CEM (BL) and SCEM).

## Slide 10
a
b
d
c
e
a
b
Notes: Figure 10 Quantification of scaling under different current density (Conditions: Feed solution = seawater brine, cell pairs = 3, membrane = SCEM, current density = 15 (BL), 12 and 9 mA/cm2. AC: acid chamber; SWBC: seawater brine chamber; BC: base chamber). (a) Reduction ratio of Mg2+ and Ca2+ in BMED system treating SWB under different current density; (b) The amount of scaling in BMED system under different current density. The concentration change of Mg2+ and Ca2+ with time in (c) AC, (d) BC and (e) SWBC.

## Slide 11
a
b
d
c
e
Notes: Figure 11 (a) Conductivity change in salt chamber and (b) Voltage change with time under different current density. (c) Concentration of generated acid and base under different current density. The current efficiency and energy consumption of the entire process to produce (d) acid and (e) base under different current density. (Conditions: Feed solution = seawater brine, cell pairs = 3, membrane = SCEM, current density = 15 (BL), 12 and 9 mA/cm2).

## Slide 12
10 μm
10 μm
10 μm
a
b
c
d
Mg
Ca
Notes: Figure S 1 Characterization of CEM (Conditions: feed solution = NaCl, current density = 15 mA/cm2, cell pairs = 3). (a) SEM graph; (b) EDS map spectrum; (c) EDS elemental mapping image of Mg; (d) EDS elemental mapping image of Ca.

## Slide 13
a1
a4
b1
a2
a3
b4
b2
b3
AEM facing SWBC
BPM facing BC
CEM facing SWBC
CEM facing BC
AEM facing SWBC
BPM facing BC
SCEM facing SWBC
SCEM facing BC
Notes: Figure S2 The photo of membranes after test. BMED with CEM: (a1) AEM facing SWBC; (a2) BPM facing BC; (a3) CEM facing SWBC; (a4) CEM facing BC. BMED with SCEM: (b1) AEM facing SWBC; (b2) BPM facing BC; (b3) SCEM facing SWBC; (b4) SCEM facing BC.

## Slide 14
1 μm
1 μm
Ca
1 μm
Mg
1 μm
1 μm
Ca
1 μm
Mg
Mg(OH)2
Ca(OH)2
Scaling on
CEM facing
SWBC
Scaling on
CEM facing
BC
Mg(OH)2
1 μm
Ca
1 μm
Mg
1 μm
Mg(OH)2
Notes: Fig. S3 The morphology of crystal on (a) CEM facing SWBC and (b) CEM facing BC.

## Slide 15
+
BPM
-
-
-
-
+
+
O2
H+
H2
OH-
OH-
H+
Electrode Chamber
Na2SO4
Notes: Figure S4. Schematic experimental setup for determining the electrode resistance. (Conditions: electrode solution = 0.3 M Na2SO4, current density = 5~20 mA/cm2)

## Slide 16
Notes: Figure S5 Voltage drop of the electrode compartments as a function of direct current.(The read line is the fitting curve)

## Slide 17
a
b
c
d
Notes: Figure S6. (a) The conductivity change in salt, acid and base chamber over time. (Conditions: Feed solution = NaCl or SWB, current density = 15 mA/cm2, cell pairs = 3, membrane = CEM); (b) The relationship between chamber resistance and total resistance in the BMED system during the treatment of SWB and NaCl solutions. (c) The resistance change of membrane and chamber over time when treating NaCl. (d) The resistance change of membrane and chamber over time when treating SWB.