## Slide 1
BPM
+
AEM
CEM/SCEM
BPM
OH-
BPM
Cl-
-
+
+
+
+
+
+
-
-
-
-
-
-
EC
AC
SWBC
BC
…
BPM
EC
OH-
H+
Scaling on CEM/SCEM
facing SWBC
Scaling on CEM/SCEM
facing BC
1
2
Ca2+
Mg2+
Na+
Ca2+
Scaling on BPM
facing BC
3
Scaling: Mg(OH)2
The leakage of OH-
Water splitting
Scaling: Ca(OH)2
The transport of Mg2+/Ca2+
Scaling: Mg(OH)2, Ca(OH)2, CaCO3
The transport of Mg2+/Ca2+
OH-
OH-
1
Mg2+
Ca2+
Na+
2
3
…
H+
OH-
H+
Water splitting
(Major)
(Minor)
Leakage
Notes: Abstract diagram. Schematic illustration of mechanisms of scaling generation in BMED system (EC: electrode chamber; AC: acid chamber; SWBC: seawater brine chamber; BC: base chamber). (b) The procedure of scaling formation on both sides of CEM/SCEM. (Aeff = effective membrane area; Ilim = limiting current)

## Slide 2
+
AEM
CEM
BPM
BPM
-
AEM
CEM
BPM
AEM
CEM
BPM
Electrode Chamber
Acid Chamber
Seawater Brine Chamber
Base Chamber
-
-
-
+
+
-
-
-
+
+
-
-
-
+
+
-
-
-
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
Acid flow
Base flow
Electrode flow
Seawater brine flow
Notes: Figure 1. The configuration of lab-scale experimental BMED stack.

## Slide 3
a
b
e
c
d
Notes: Figure 2. (a) Conductivity changes in SWBC; (b) Voltage changes across the BMED system; (c) Variation of stack resistance, chamber resistance and membrane resistance; (d) pH change in SWBC; (e) Concentration of generated acid and base during BMED treating different solutions (SWB, seawater brine; NaCl, the sodium chloride solution with the same conductivity as SWB).

## Slide 4
10 μm
10 μm
10 μm
Ca
10 μm
Mg
10 μm
Ca
10 μm
Mg
Ca
10 μm
Mg
10 μm
Mg
Ca
10 μm
10 μm
10 μm
a2
a3
a4
AEM facing SWBC
BPM facing BC
CEM facing SWBC
CEM facing BC
NaCl
a1
a5
a6
b2
b3
b4
b1
b5
b6
c2
c3
c4
c1
c5
c6
SWB
NaCl
SWB
NaCl
SWB
NaCl
SWB
d2
d3
d4
d1
d5
d6
10 μm
Notes: Figure 3. Characterization of IEMs. AEM facing SWBC: Photograph after tests in (a1) NaCl and (a2) SWB; (a3) SEM diagram; EDS elemental mapping image of (a4) Mg and (a5) Ca; (a6) EDS map spectrum. CEM facing SWBC: Photograph after tests in (b1) NaCl and (b2) SWB; (b3) SEM diagram; EDS elemental mapping image of (b4) Mg and (b5) Ca; (b6) EDS map spectrum. CEM facing BC: Photograph after tests in (c1) NaCl and (c2) SWB; (c3) SEM diagram; EDS elemental mapping image of (c4) Mg and (c5) Ca; (c6) EDS map spectrum. BPM facing BC: Photograph after tests in (d1) NaCl and (d2) SWB; (d3) SEM diagram; EDS elemental mapping image of (d4) Mg and (d5) Ca; (d6) EDS map spectrum. (AC: acid chamber; SWBC: seawater brine chamber; BC: base chamber).

## Slide 5
a
b
Notes: Figure 4. Quantification of scaling in BMED system. (a) The amount of scaling and (b) Reduction ratio of Mg2+ and Ca2+

## Slide 6
Notes: Figure 5. Concentration of Ca2+ and Mg2+ in (a) SWBC and (b) BC; (c) The transport number of counter-ions of pristine CEM, scaled CEM, CEM-Ca and CEM-Mg

## Slide 7
OH-
CEM
SWBC
BC
Mg2+
Ca2+
OH-
Divalent ion transport
Scaling on CEM facing BC
Mg2+
Ca2+
Mg(OH)2 ↓
Ca(OH)2 ↓
CaCO3 ↓
CEM
SWBC
BC
Mg(OH)2 ↓
Ca(OH)2 ↓
CaCO3 ↓
H2O
OH- + H+
OH-
Mg2+
Ca2+
CEM
SWBC
BC
Mg(OH)2 ↓
Ca(OH)2 ↓
CaCO3 ↓
H2O
OH- + H+
Mg2+
Ca2+
H2O
OH- + H+
Water splitting on CEM facing BC
OH- accumulated in SWBC
Scaling on CEM facing SWBC
Water splitting on CEM facing SWBC
Scaling was enhanced
OH-
OH-
Notes: Figure 6. Schematic diagram of scaling formation mechanisms on CEM.

## Slide 8
CEM
SWBC
BC
BPM
-
-
-
-
-
-
+
+
+
+
+
Mg2+
OH-
Mg2+
OH-
Ca2+
Ca2+
Ca2+
Ca(OH)2 ↓
Notes: Figure 7. (a) schematic diagram of scaling formation on BPM.

## Slide 9
Notes: Figure 8. Performance change before scaling, after scaling and after cleaning.

## Slide 10
SI

## Slide 11
Section S1. The composition of model seawater brine
Notes: Table S1. The composition of model SWB

## Slide 12
Section S2. System electrical resistance calculation
+
BPM
-
-
-
-
+
+
O2
H+
H2
OH-
OH-
H+
Electrode Chamber
Na2SO4
Notes: Figure S1. Schematic experimental setup for determining the electrode resistance. (Conditions: electrode solution = 0.3 M Na2SO4, current density = 5~20 mA/cm2)

## Slide 13
Section S2. System electrical resistance calculation
Notes: Figure S2 The change of voltage drop of the electrode compartment as a function of direct current. (The read line is the fitting curve)

## Slide 14
Section S4: BMED acid/base conductivity, acid/base production rate, and SEC
Notes: Figure S3 The conductivity change of acid chamber and base chamber. (AC: acid chamber; BC: base chamber)

## Slide 15
Section S4: BMED acid/base conductivity, acid/base production rate, and SEC
a
b
Notes: Figure S4. The acid and base production rate change with time

## Slide 16
Section S4: BMED acid/base conductivity, acid/base production rate, and SEC
Notes: Figure S4. The energy consumption of the entire process to produce acid and base.

## Slide 17
Section S5. Scaling formation in chambers
Brine
Base
Acid
(a2) Solutions at the end of testing (NaCl)
(a1) Solutions at the beginning of testing (NaCl)
(b1) Solutions at the beginning of testing (SWB)
(b2) Solutions at the end of testing (SWB)
Brine
Base
Acid
Brine
Base
Acid
Brine
Base
Acid
Notes: Figure S5. Photos of solution at the beginning of testing and at the end of testing (NaCl & SWB).

## Slide 18
Section S5. Scaling formation in chambers
Notes: Table S2. Turbidity of solutions at the beginning and end of testing.

## Slide 19
Section S6. Characterization of pristine membranes and membranes after NaCl tests
10 μm
10 μm
10 μm
a1
a2
b1
b2
c1
c2
Notes: Figure S6. Characterization of pristine IEMs. AEM: (a1) SEM image; (a2) EDS map spectrum. CEM: (b1) SEM image; (b2) EDS map spectrum. BPM (AEL): (c1) SEM image; (c2) EDS map spectrum

## Slide 20
Section S6. Characterization of pristine membranes and membranes after NaCl tests
10 μm
10 μm
10 μm
10 μm
a1
a2
b1
b2
c1
c2
d1
d2
Notes: Figure S7. Characterization of IEMs after BMED tests treating NaCl. AEM facing SWBC: (a1) SEM image; (a2) EDS map spectrum. CEM facing SWBC: (b1) SEM image; (b2) EDS map spectrum. CEM facing BC: (c1) SEM image; (c2) EDS map spectrum. BPM facing BC: (d1) SEM image; (d2) EDS map spectrum

## Slide 21
Section S7. The composition of scaling
Scaling on CEM facing SWBC
100 μm
Mg
100 μm
100 μm
Ca
a
b
c
d
Notes: Figure S8. The morphology of deposits on CEM facing SWBC (a) SEM image; (b) EDS map spectrum; EDS elemental mapping image of (c) Mg and (d) Ca;

## Slide 22
Mg(OH)2
CaCO3.
1 μm
1 μm
1 μm
Ca
Mg
Ca
Mg
1 μm
1 μm
1 μm
Scaling on CEM facing BC
Mg(OH)2
Section S7. The composition of scaling
a1
a4
a3
a2
b1
b4
b3
b2
Ca
Notes: Figure S9. The morphology of deposits on CEM facing BC: (a1)(b1) SEM images; (a2)(b2) EDS map spectrum; EDS elemental mapping image of (a3)(b3) Mg and (a4)(b4) Ca.

## Slide 23
Section S7. The composition of scaling
Brucite Mg(OH)2
Calcite CaCO3
Portlandite Ca(OH)2
NaCl
Notes: Figure S10. X-ray diffraction spectra for the precipitates collected in the stack.

## Slide 24
Section S7. The method to quantify scaling
Notes: Figure S11. The concentration change of Mg2+ and Ca2+ in the acid chamber.

## Slide 25
Section S8. The calculation of transport number
V
Multimeter
0.2M NaOH
0.1M NaOH
Notes: Figure S12. The stack diagram

## Slide 26
1 μm
1 μm
1 μm
1 μm
1 μm
1 μm
Ca
Mg
Ca
Mg
a1
a2
a3
a4
b1
b2
b3
b4
Cross-section
Surface
Cross-section
Surface
Notes: Figure S13 The SEM graph and EDS map spectrum of cross-section of membranes (White line is the dividing line of cross-section and membrane surface). Cross-section of CEM after tests: (a1) SEM diagram; (a2) EDS map spectrum; (a3) EDS elemental mapping image of Ca; (a4) EDS elemental mapping image of Mg. Cross-section of BPM(AEL) after tests: (b1) SEM diagram; (b2) EDS map spectrum; (b3) EDS elemental mapping image of Ca; (b4) EDS elemental mapping image of Mg.