## Slide 1
Chapter 1
As constant current is applied, voltage is proportional to the stack resistance. To analyze the reason why voltage remained high, we can explore the stack resistance. The resistance can be expressed:
where is the number of repeating units, is the effective membrane area (m2), is the anion exchange membrane resistance (Ωm2), is the cation exchange membrane resistance (Ωm2), is the bipolar membrane resistance (Ωm2), is the thickness of the acid chamber (m), is the thickness of the base chamber (m), is thickness of the seawater brine chamber (m), is the acid chamber conductivity (S/m) , is the base chamber conductivity (S/m), is the seawater brine chamber conductivity (S/m) and is the electrode resistance (Ω).
Rmembrane
Rchamber

## Slide 2
In that case, we can compare the resistance of membrane & chamber when BMED treats NaCl and SWB.
We just need to measure the conductivity of acid/base/SWB chambers and measure the resistance of electrode.
This figure illustrates the voltage change of electrode when current changes.
As the current density used is 15 mA/cm2, I=0.106A, U=4.58V, Rele=43.04511Ω
Chart: I (A)
| 3.4400001168251003E-2 | 4.14000004529953E-2 | 4.8500001430511502E-2 | 5.5599998682737399E-2 | 6.2700003385543795E-2 | 6.9899998605251298E-2 | 7.8100003302097307E-2 | 8.5299998521804796E-2 | 9.2399999499320998E-2 | 9.9399998784065205E-2 | 0.10639999806880999 | 0.11339999735355399 | 0.120300002396107 | 0.12729999423027 | 0.13420000672340399 | 0.141100004315376
U,V | 3.4295 | 3.5673 | 3.6931 | 3.8153 | 3.9299 | 4.0408 | 4.1646 | 4.2704 | 4.3783 | 4.478 | 4.5812 | 4.6898 | 4.7884 | 4.8816 | 4.9817 | 5.0823
Fig. Voltage drop of the electrode compartments as a function of direct current

## Slide 3
Fig. Conductivity change in the acid, base and SWB chambers
The conductivity of chambers are also measured.

## Slide 4
Chart: Time (h)
| 0 | 0.5 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9
RchamberT,Ω | 258.9698 | 120.1333 | 78.8501 | 49.065 | 37.4931 | 30.8157 | 27.4194 | 25.3352 | 23.3517 | 21.8339 | 20.6256
RmemT, Ω | 162.1447 | 137.6385 | 196.5179 | 251.7679 | 240.1097 | 246.8528 | 277.4603 | 268.4929 | 252.3826 | 250.6985 | 237.7001
Fig. Resistance of membrane and chamber when treating SWB and NaCl
The membrane resistance attributed to the total resistance and total voltage.
Chart: Time, h
| 0 | 0.5 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9
RchamberT,Ω | 293.5081 | 125.7189 | 81.1348 | 49.4111 | 36.7614 | 29.9694 | 25.7802 | 22.9552 | 20.9298 | 19.422 | 18.2956
RmemT, Ω | 46.6362 | 37.58 | 36.2055 | 34.3201 | 33.3702 | 32.8463 | 32.6422 | 32.2405 | 32.5632 | 32.7446 | 32.7421
SWB
NaCl

## Slide 5
RT,1=Rmem,1+Rcham,1+Rele
RT,2=Rmem,2+Rcham,2+Rele
Let Rcham,1= Rcham,2
Δ RT= Δ Rmem
Membrane resistance
Fig. The relationship pf chamber resistance and total resistance

## Slide 6
In the experiment, we also find that pH of SWB chamber increased significantly after 30 min.
When treating NaCl, pH of salt solution continued to decrease because the transport speed of proton was fast. This is the normal phenomenon.

## Slide 7
10 μm
10 μm
10 μm
10 μm
Cross-section
Surface
Cross-section of BPM

## Slide 8
10 μm
10 μm
10 μm
10 μm
Cross-section
Surface
Cross-section of CEM

## Slide 9
Chapter 2
0 ppm Mg 10 ppm Ca
10 μm
10 μm
FSWB
FB
Scaling

## Slide 10
0 ppm Mg 1 ppm Ca
10 μm
10 μm
FSWB
FB
Scaling