## Slide 1: Experiment Plan 1
Salt solution of known composition
e.g., 59 g/L Na +50 ppm Mg+50 ppm Ca
BMED
Initial pH
Current density
Flow rate
Optimal parameters
Real SWB
(NaCl, Ca, Mg, Sr, SO4 …)
BMED
Scaling?
YES
Reduce
Ca, Mg
Scaling?
Max. [Ca], [Mg]
Make some adjustments up and down
Pretreatment
Adding NaOH until Mg/Ca concentration reach the target
Prepare a solution of known composition
Run BMED under different conditions and test whether there is scaling
With the optimal conditions, use real SWB and do pretreatment and test in BMED

## Slide 2: Experiment Plan 2
Real SWB
(NaCl, Ca, Mg, Sr, SO4 …)
BMED
Current density
Flow rate
Optimal parameters
Scaling?
Max. Ca Mg
Seawater desalination brine composition
Component | SWB composition [mg/L]
NaCl | 59000
K+ | 700
Ca2+ | 830
Mg2+ | 2600
SO42- | 5400
Sr2+ | 16
Directly use SWB and add NaOH to reduce Mg/Ca. The final salt solution is used for BMED.
Test whether there is
Get the max. [Ca], [Mg] under the optimal conditions
Pretreatment
Adding NaOH until Mg/Ca concentration reach the target

## Slide 3
2. Current Density
Impact on OH⁻ Generation:
  Related to the rate of water dissociation at the BPM, leading to higher OH⁻ concentrations near the BPM.
  Excess OH⁻ accelerates the precipitation of divalent ion hydroxides (e.g., Ca(OH)₂, Mg(OH)₂).
Impact on divalent ion Transport:
  Higher current density enhances the migration of Ca²⁺ and Mg²⁺ toward the membrane.
  If the current exceeds the limiting current density, concentration polarization can occur, leading to supersaturation and scaling.
1. Feed Solution Composition
Impact on Ksp
  The concentration in salt solution directly affects scaling
3. pH of the Feed Solution
Initial pH
  As the leakage of OH- to salt chamber, there is scaling on CEM facing salt chamber. A lower pH may help to neutralize the leakage.

## Slide 4
4. Flow Rate and Hydrodynamics
Turbulence:
  Higher flow rates enhance mixing and reduce ion concentration polarization near the BPM, mitigating scaling.
Boundary Layer Thickness:
  Lower flow rates increase the boundary layer thickness, leading to localized supersaturation and precipitation.
5. Membrane type
Impact on ion transport
  Normal CEM allow all ions to pass through, while selective CEM will prevent most divalent ions
  Related to the scaling on membrane facing base chamber.
Impact on OH- leakage
  Whether it can prevent OH- leakage

## Slide 5
pH
7,8,9,10
CD [mA/cm2]
9,12,15
FR[L/min]
0.2, 0.5, 0.8
Variables