## Slide 1: Experiment Plan 1
Salt solution of known composition
e.g., 59 g/L Na +50 ppm Mg+50 ppm Ca
BMED
Initial pH
Current density
Flow rate
Optimal parameters
Real SWB
(NaCl, Ca, Mg, Sr, SO4 …)
BMED
Scaling?
YES
Reduce
Ca, Mg
Scaling?
Max. [Ca], [Mg]
Make some adjustments up and down
Pretreatment
Adding NaOH until Mg/Ca concentration reach the target
Prepare a solution of known composition
Run BMED under different conditions and test whether there is scaling
With the optimal conditions, use real SWB and do pretreatment and test in BMED

## Slide 2: Experiment Plan 2
Real SWB
(NaCl, Ca, Mg, Sr, SO4 …)
BMED
Current density
Flow rate
Optimal parameters
Scaling?
Max. Ca Mg
Seawater desalination brine composition
Component | SWB composition [mg/L]
NaCl | 59000
K+ | 700
Ca2+ | 830
Mg2+ | 2600
SO42- | 5400
Sr2+ | 16
Directly use SWB and add NaOH to reduce Mg/Ca. The final salt solution is used for BMED.
Test whether there is
Get the max. [Ca], [Mg] under the optimal conditions
Pretreatment
Adding NaOH until Mg/Ca concentration reach the target

## Slide 3
1. Current Density
Impact on OH⁻ Generation:
  Higher current densities increase the rate of water dissociation at the BPM, leading to higher OH⁻ concentrations near the BPM.
  Excess OH⁻ accelerates the precipitation of divalent ion hydroxides (e.g., Ca(OH)₂, Mg(OH)₂).
Impact on Ion Transport:
  Higher current density enhances the migration of Ca²⁺ and Mg²⁺ toward the membrane.
  If the current exceeds the limiting current density, concentration polarization can occur, leading to supersaturation and scaling.
2. Feed Solution Composition
Divalent Ion Concentrations (Ca²⁺, Mg²⁺):
  High concentrations increase the likelihood of exceeding solubility limits near the BPM.
Co-ion Effects:
  Presence of anions like CO₃²⁻ or SO₄²⁻ can lead to the formation of insoluble salts (e.g., CaCO₃, MgSO₄).
Buffering Capacity:
  Solutions with poor buffering may experience localized pH spikes near the membrane, exacerbating scaling.

## Slide 4
3. pH of the Feed Solution
Initial pH:
  A lower initial pH reduces OH⁻ concentration at the start but may not prevent localized scaling near the BPM where pH spikes.
pH Gradient:
  The extent of pH change across the system influences OH⁻ availability for scaling reactions.
4. Flow Rate and Hydrodynamics
Turbulence:
  Higher flow rates enhance mixing and reduce ion concentration polarization near the BPM, mitigating scaling.
Boundary Layer Thickness:
  Lower flow rates increase the boundary layer thickness, leading to localized supersaturation and precipitation.

## Slide 5
pH
7,8,9,10
CD [mA/cm2]
9,12,15
FR[L/min]
0.2, 0.5, 0.8
Variables